## Slide 1
08 · Solid Deformation
Follow a complete tensile test
Stress-Strain Curves
Read proportional response, elastic recovery, yielding, ultimate tensile stress, necking, and fracture from one engineering stress–strain curve.
POSITION
Lesson 4 of 7 in Solid Deformation
PLAN
16 slides in the 45-minute core run, about 45 minutes of it
LESSON PAGE
https://giophysics.com/chapter-14/stress-strain-curves/
Built by GioPhysics from the lesson's own page. Every word on these slides is the lesson's; nothing here is re-authored. Teaching material, not an awarding body's document.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
1 / 31
Notes: [Lesson] Solid Deformation — Stress-Strain Curves. Lesson 4 of 7.
[Intro] Read proportional response, elastic recovery, yielding, ultimate tensile stress, necking, and fracture from one engineering stress–strain curve.
[Source] https://giophysics.com/chapter-14/stress-strain-curves/
[Disclaimer] Built by GioPhysics from the lesson's own page. Every word on these slides is the lesson's; nothing here is re-authored. Teaching material, not an awarding body's document.

## Slide 2
THINK FIRST
One metal takes twice the stress before it fails; the other stretches ten times further. Which do you build the crash barrier from?
Take answers before you click — the point is the commitment
Two test bars, two curves and a purchasing decision.
THE ANSWER
The one that stretches. A barrier's job is to absorb the energy of an impact, and the energy absorbed per unit volume is the AREA under the stress–strain curve — a long low curve encloses far more of it than a short tall one. Strength is the height of the curve; toughness is its area.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
2 / 31
Notes: [Phase] Starter: Recall what this lesson stands on (minutes 0–5 of 45)
[Hook] One metal takes twice the stress before it fails; the other stretches ten times further. Which do you build the crash barrier from? Two test bars, two curves and a purchasing decision.
[Answer] The one that stretches. A barrier's job is to absorb the energy of an impact, and the energy absorbed per unit volume is the AREA under the stress–strain curve — a long low curve encloses far more of it than a short tall one. Strength is the height of the curve; toughness is its area.

## Slide 3
EXPLAINED SIMPLY
In one sentence
Introduce the idea — The big idea and the definition
A stress-strain curve shows how a material deforms as stress increases, from elastic response through yielding and finally fracture.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
3 / 31
Notes: [Phase] Introduce the idea: The big idea and the definition (minutes 5–13 of 45)
[Definition] A stress-strain curve shows how a material deforms as stress increases, from elastic response through yielding and finally fracture.

## Slide 4
EXPLAINED SIMPLY
What that looks like
Introduce the idea — The big idea and the definition
FOR EXAMPLE
On a steel test curve, the first straight section shows elastic behaviour; after yielding, removing the load leaves permanent strain.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
4 / 31
Notes: [Phase] Introduce the idea: The big idea and the definition (minutes 5–13 of 45)
[Worked illustration] On a steel test curve, the first straight section shows elastic behaviour; after yielding, removing the load leaves permanent strain.

## Slide 5
THE BIG IDEA
Follow a complete tensile test
Introduce the idea — The big idea and the definition
A tensile test reveals several different limits. The initial gradient gives Young modulus.
Past the elastic limit, unloading leaves plastic strain. The highest engineering stress is the ultimate tensile stress; fracture can occur later at a lower engineering stress after necking.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
5 / 31
Notes: [Phase] Introduce the idea: The big idea and the definition (minutes 5–13 of 45)
[Big idea] A tensile test reveals several different limits. The initial gradient gives Young modulus. Past the elastic limit, unloading leaves plastic strain. The highest engineering stress is the ultimate tensile stress; fracture can occur later at a lower engineering stress after necking.

## Slide 6
THE PHYSICS · 1 OF 3
Proportional region
Build the model — The formulae, one at a time, in plain English
Stress is proportional to strain, so the graph is straight and E is constant.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
6 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Section] Stress is proportional to strain, so the graph is straight and E is constant.

## Slide 7
THE PHYSICS · 2 OF 3
Plastic region
Build the model — The formulae, one at a time, in plain English
After yielding, large strain can occur with permanent rearrangement inside the material.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
7 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Section] After yielding, large strain can occur with permanent rearrangement inside the material.

## Slide 8
THE PHYSICS · 3 OF 3
UTS then fracture
Build the model — The formulae, one at a time, in plain English
Engineering stress may fall during necking because it uses the original area, even while the narrowed section approaches fracture.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
8 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Section] Engineering stress may fall during necking because it uses the original area, even while the narrowed section approaches fracture.

## Slide 9
FORMULA 1 OF 3
Initial gradient
Build the model — The formulae, one at a time, in plain English
E = Δσ/Δε
Use the linear elastic region
IN PLAIN ENGLISH
Read the Young modulus off the straight first part of a stress–strain graph.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
9 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Formula] Initial gradient: E = Δσ/Δε
[In plain English] Read the Young modulus off the straight first part of a stress–strain graph.
[Note] Use the linear elastic region

## Slide 10
FORMULA 2 OF 3
Ultimate tensile stress
Build the model — The formulae, one at a time, in plain English
UTS = max(σ)
Top of the engineering curve
IN PLAIN ENGLISH
The highest stress a material bears before it starts to fail — the peak of the curve.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
10 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Formula] Ultimate tensile stress: UTS = max(σ)
[In plain English] The highest stress a material bears before it starts to fail — the peak of the curve.
[Note] Top of the engineering curve

## Slide 11
FORMULA 3 OF 3
Toughness
Build the model — The formulae, one at a time, in plain English
energy/volume = ∫ σ dε
Area to fracture
IN PLAIN ENGLISH
How much energy each bit of material absorbs before breaking — the whole area under the stress–strain curve.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
11 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Formula] Toughness: energy/volume = ∫ σ dε
[In plain English] How much energy each bit of material absorbs before breaking — the whole area under the stress–strain curve.
[Note] Area to fracture

## Slide 12
THE PICTURE
One tensile test, end to end
Drawn for this lesson
An engineering stress–strain curve: a straight section climbing to a marked limit of proportionality at 250 MPa, then a bending region that rises more slowly to a marked peak at 430 MPa, then a fall to where the plot stops. The regions along the bottom are named elastic, plastic flow and necking.
The live version of this figure — click here
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
12 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Figure] An engineering stress–strain curve: a straight section climbing to a marked limit of proportionality at 250 MPa, then a bending region that rises more slowly to a marked peak at 430 MPa, then a fall to where the plot stops. The regions along the bottom are named elastic, plastic flow and necking.

## Slide 13
WATCH OUT
The common trap
Check and misconception — The quick check and the trap
Ultimate tensile stress is the maximum engineering stress, not necessarily the stress at the fracture point.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
13 / 31
Notes: [Phase] Check and misconception: The quick check and the trap (minutes 35–41 of 45)
[Misconception] Ultimate tensile stress is the maximum engineering stress, not necessarily the stress at the fracture point.

## Slide 14
WORKED EXAMPLE 1 OF 2 · EASY
The question
Easy
Worked examples — I do, we do — one step revealed at a time
On a stress–strain graph, the linear section passes through (0.002, 400 MPa). Find the Young modulus.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
14 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Question] On a stress–strain graph, the linear section passes through (0.002, 400 MPa). Find the Young modulus.
[Answer] E = 200 GPa

## Slide 15
WORKED EXAMPLE 1 OF 2 · EASY · THE WORKING
How to solve it
Easy
Worked examples — I do, we do — one step revealed at a time
On a stress–strain graph, the linear section passes through (0.002, 400 MPa). Find the Young modulus.
1.
E = σ/ε = 400 × 10⁶ ÷ 0.002.
2.
E = 2.0 × 10¹¹ Pa = 200 GPa.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
15 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Reveal] One click per step. The class works each line before the next appears.
[Step 1] E = σ/ε = 400 × 10⁶ ÷ 0.002.
[Step 2] E = 2.0 × 10¹¹ Pa = 200 GPa.

## Slide 16
WORKED EXAMPLE 1 OF 2 · EASY
Answer
Easy
Worked examples — I do, we do — one step revealed at a time
E = 200 GPa
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
16 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Answer] E = 200 GPa

## Slide 17
WORKED EXAMPLE 2 OF 2 · MEDIUM
The question
Medium
Worked examples — I do, we do — one step revealed at a time
A material has stress 160 MPa at strain 8.0 × 10⁻⁴ in its linear region. Find Young modulus.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
17 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Question] A material has stress 160 MPa at strain 8.0 × 10⁻⁴ in its linear region. Find Young modulus.
[Answer] E = 2.0 × 10¹¹ Pa = 200 GPa

## Slide 18
WORKED EXAMPLE 2 OF 2 · MEDIUM · THE WORKING
How to solve it
Medium
Worked examples — I do, we do — one step revealed at a time
A material has stress 160 MPa at strain 8.0 × 10⁻⁴ in its linear region. Find Young modulus.
1.
Convert 160 MPa = 160 × 10⁶ Pa.
2.
Use E = σ/ε.
3.
E = (160 × 10⁶)/(8.0 × 10⁻⁴).
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
18 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Reveal] One click per step. The class works each line before the next appears.
[Step 1] Convert 160 MPa = 160 × 10⁶ Pa.
[Step 2] Use E = σ/ε.
[Step 3] E = (160 × 10⁶)/(8.0 × 10⁻⁴).

## Slide 19
WORKED EXAMPLE 2 OF 2 · MEDIUM
Answer
Medium
Worked examples — I do, we do — one step revealed at a time
E = 2.0 × 10¹¹ Pa = 200 GPa
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
19 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Answer] E = 2.0 × 10¹¹ Pa = 200 GPa

## Slide 20
SPOT THE MISTAKE
One line here is wrong
The whole working is up — find the bad line before you click
1.
The straight section passes through a strain of 0.2 % at a stress of 400 MPa.
2.
Young modulus is the gradient there: E = σ/ε.
3.
E = 400 × 10⁶ ÷ 0.2 = 2.0 × 10⁹ Pa = 2.0 GPa.
4.
So the material has E = 2.0 GPa.
LINE 3 IS WRONG
0.2 % was typed in as 0.2. A percentage is already a fraction of a hundred, so 0.2 % is 0.002, and dropping that puts E out by a factor of 500 — enough to turn a steel into a plastic without the number ever looking odd on its own.
IT SHOULD SAY
E = 400 × 10⁶ ÷ 0.002 = 2.0 × 10¹¹ Pa = 200 GPa.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
20 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Spot the mistake] The working is complete and one line of it is wrong. Let the room hunt: one click names the line, a second shows it done correctly.
[Line 3 is wrong] 0.2 % was typed in as 0.2. A percentage is already a fraction of a hundred, so 0.2 % is 0.002, and dropping that puts E out by a factor of 500 — enough to turn a steel into a plastic without the number ever looking odd on its own.
[It should say] E = 400 × 10⁶ ÷ 0.002 = 2.0 × 10¹¹ Pa = 200 GPa.

## Slide 21
PREDICT · TAKE THE VOTE
Commit before you are told
Hands up for each option, then click
Where on this curve does the specimen actually break?
A At the peak — that is the most stress the material can stand
B At the right-hand end of the plot, at a lower stress than the peak
C At the limit of proportionality, where the line stops being straight
An engineering stress–strain curve: a straight section climbing to a marked limit of proportionality at 250 MPa, then a bending region that rises more slowly to a marked peak at 430 MPa, then a fall to where the plot stops. The regions along the bottom are named elastic, plastic flow and necking.
The live version of this figure — click here
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
21 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Predict] Where on this curve does the specimen actually break?
[Options] A At the peak — that is the most stress the material can stand B At the right-hand end of the plot, at a lower stress than the peak C At the limit of proportionality, where the line stops being straight
[Figure] An engineering stress–strain curve: a straight section climbing to a marked limit of proportionality at 250 MPa, then a bending region that rises more slowly to a marked peak at 430 MPa, then a fall to where the plot stops. The regions along the bottom are named elastic, plastic flow and necking.

## Slide 22
PREDICT · THE OUTCOME
What actually happens
Ask the room who changed their mind, and why
B At the right-hand end of the plot, at a lower stress than the peak
WHY
The peak is the ultimate tensile STRESS, not the moment of failure. Past it the specimen necks: a narrow waist carries the load while the graph goes on dividing by the original area, so the plotted stress falls even though the material at the waist is being pulled harder than ever. Fracture comes at the end of that fall.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
22 / 31
Notes: [Phase] Build the model: The formulae, one at a time, in plain English (minutes 13–22 of 45)
[Answer] B — At the right-hand end of the plot, at a lower stress than the peak. The peak is the ultimate tensile STRESS, not the moment of failure. Past it the specimen necks: a narrow waist carries the load while the graph goes on dividing by the original area, so the plotted stress falls even though the material at the waist is being pulled harder than ever. Fracture comes at the end of that fall.

## Slide 23
QUICK CHECK
Decide before the answer goes up
Check and misconception — The quick check and the trap
Where is Young modulus found on a stress–strain graph?
A
The gradient of the initial straight section
B
The total area under the graph
C
The strain coordinate at fracture
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
23 / 31
Notes: [Phase] Check and misconception: The quick check and the trap (minutes 35–41 of 45)
[Question] Where is Young modulus found on a stress–strain graph?
[Options] A The gradient of the initial straight section B The total area under the graph C The strain coordinate at fracture

## Slide 24
QUICK CHECK · THE ANSWER
The answer, and why
Check and misconception — The quick check and the trap
A The gradient of the initial straight section
HOW TO GET THERE
E = σ/ε in the linear elastic region, so it is the initial stress–strain gradient.
WHY THE OTHERS TEMPT
A Right. E = σ/ε, and that ratio is only constant where the graph is straight, so E is the gradient of the initial straight section.
B The area under a stress–strain graph is energy per unit volume — the toughness. A useful number, but it comes out in J m⁻³, not in pascals.
C The strain at fracture tells you how far the material stretched before it broke, which is its ductility. Stiffness and ductility are separate questions and a material can be high in one and low in the other.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
24 / 31
Notes: [Phase] Check and misconception: The quick check and the trap (minutes 35–41 of 45)
[Question] Where is Young modulus found on a stress–strain graph?
[Option by option] A: Right. E = σ/ε, and that ratio is only constant where the graph is straight, so E is the gradient of the initial straight section. B: The area under a stress–strain graph is energy per unit volume — the toughness. A useful number, but it comes out in J m⁻³, not in pascals. C: The strain at fracture tells you how far the material stretched before it broke, which is its ductility. Stiffness and ductility are separate questions and a material can be high in one and low in the other.
[Answer] A — The gradient of the initial straight section
[Why] E = σ/ε in the linear elastic region, so it is the initial stress–strain gradient.
[Reveal] One click for the answer, then one for the reason.

## Slide 25
EXTENSION 1 OF 2 · HARD
The question
Hard
Worked examples — I do, we do — one step revealed at a time
From a stress–strain curve: proportional limit 250 MPa, UTS 430 MPa, fracture at strain 0.15. Sketch-read: which regions are elastic, plastic, and necking?
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
25 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Question] From a stress–strain curve: proportional limit 250 MPa, UTS 430 MPa, fracture at strain 0.15. Sketch-read: which regions are elastic, plastic, and necking?
[Answer] Elastic to 250 MPa; plastic 250→430 MPa; necking beyond the peak

## Slide 26
EXTENSION 1 OF 2 · HARD · THE WORKING
How to solve it
Hard
Worked examples — I do, we do — one step revealed at a time
From a stress–strain curve: proportional limit 250 MPa, UTS 430 MPa, fracture at strain 0.15. Sketch-read: which regions are elastic, plastic, and necking?
1.
Up to 250 MPa the line is straight — elastic (and Hookean).
2.
From 250 MPa to the 430 MPa peak the material yields and work-hardens — plastic flow.
3.
Past the UTS the sample necks: stress on the engineering axis falls until fracture at ε = 0.15.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
26 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Reveal] One click per step. The class works each line before the next appears.
[Step 1] Up to 250 MPa the line is straight — elastic (and Hookean).
[Step 2] From 250 MPa to the 430 MPa peak the material yields and work-hardens — plastic flow.
[Step 3] Past the UTS the sample necks: stress on the engineering axis falls until fracture at ε = 0.15.

## Slide 27
EXTENSION 1 OF 2 · HARD
Answer
Hard
Worked examples — I do, we do — one step revealed at a time
Elastic to 250 MPa; plastic 250→430 MPa; necking beyond the peak
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
27 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Answer] Elastic to 250 MPa; plastic 250→430 MPa; necking beyond the peak

## Slide 28
EXTENSION 2 OF 2 · CHALLENGING
The question
Challenging
Worked examples — I do, we do — one step revealed at a time
Material P fractures at strain 0.02 with UTS 900 MPa; material Q at strain 0.25 with UTS 500 MPa. Which is tougher, and which would you choose for a crash structure? Estimate using triangle/rectangle areas.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
28 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Question] Material P fractures at strain 0.02 with UTS 900 MPa; material Q at strain 0.25 with UTS 500 MPa. Which is tougher, and which would you choose for a crash structure? Estimate using triangle/rectangle areas.
[Answer] Q (≈ 88 vs ≈ 9 MJ/m³) — strength is not toughness

## Slide 29
EXTENSION 2 OF 2 · CHALLENGING · THE WORKING
How to solve it
Challenging
Worked examples — I do, we do — one step revealed at a time
Material P fractures at strain 0.02 with UTS 900 MPa; material Q at strain 0.25 with UTS 500 MPa. Which is tougher, and which would you choose for a crash structure? Estimate using triangle/rectangle areas.
1.
Toughness ≈ area under the curve. P: ~½ × 900 MPa × 0.02 ≈ 9 MJ/m³.
2.
Q: roughly 500 MPa × 0.25 × 0.7 ≈ 88 MJ/m³ — ten times tougher.
3.
P is stronger but brittle; Q absorbs far more energy before failing — choose Q for crash zones.
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
29 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Reveal] One click per step. The class works each line before the next appears.
[Step 1] Toughness ≈ area under the curve. P: ~½ × 900 MPa × 0.02 ≈ 9 MJ/m³.
[Step 2] Q: roughly 500 MPa × 0.25 × 0.7 ≈ 88 MJ/m³ — ten times tougher.
[Step 3] P is stronger but brittle; Q absorbs far more energy before failing — choose Q for crash zones.

## Slide 30
EXTENSION 2 OF 2 · CHALLENGING
Answer
Challenging
Worked examples — I do, we do — one step revealed at a time
Q (≈ 88 vs ≈ 9 MJ/m³) — strength is not toughness
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
30 / 31
Notes: [Phase] Worked examples: I do, we do — one step revealed at a time (minutes 22–35 of 45)
[Answer] Q (≈ 88 vs ≈ 9 MJ/m³) — strength is not toughness

## Slide 31
SOLID DEFORMATION
Where to go next
Plenary — What to take away, what to practise next
Next
8.5 Elastic, Plastic, Brittle & Ductile Behaviour
https://giophysics.com/chapter-14/elastic-plastic-brittle-ductile-behaviour/
Lesson
This lesson on giophysics.com
https://giophysics.com/chapter-14/stress-strain-curves/
Live
The live, interactive version of these slides
https://giophysics.com/chapter-14/presentation/?lesson=curve
Chapter
All Solid Deformation lessons
https://giophysics.com/chapter-14/
PDF
Download the lesson PDF
https://giophysics.com/downloads/14-4-stress-strain-curves.pdf
SOLID DEFORMATION · STRESS-STRAIN CURVES
GIOPHYSICS LESSON
Solid Deformation — Stress-Strain Curves. Built by GioPhysics from the lesson's own copy; nothing on these slides is re-authored.
31 / 31
Notes: [Phase] Plenary: What to take away, what to practise next (minutes 41–45 of 45)
[Interactive] The graphs and the circuit topology on these slides are frozen. The live version at https://giophysics.com/chapter-14/presentation/?lesson=curve moves them.